### 中華民國田徑協會國家級400公尺標準田徑場跑道面層規範

2016.09

- 面層厚度：跑道於建造完成時，面層厚度須均勻一致，跑道面層平均厚度不可少於13mm；但須要加厚的區域(如三級跳遠、跳高起跳區、撐竿跳、標槍及障礙賽池底斜面等局部須特別加厚)，其詳細規定如下：

加厚區：

| 項次 | 跑道及助跑道 | 厚度 | 範圍（長度） |
| --- | --- | --- | --- |
| 1 | 三級跳遠助跑道 | 20 mm | 助跑道之最後13m |
| 2 | 跳高起跳區 | 20 mm | 助跑道之最後3m |
| 3 | 撐竿跳助跑道 | 20 mm | 助跑道之最後8m |
| 4 | 標槍助跑道 | 20 mm | 助跑道之最後8m及投擲弧線前區域 |
| 5 | 障礙賽池底斜面 | 25 mm | 全部 |

- 面層測試：田徑場跑道材質須送國際田徑總會認可之實驗室測試，測試結果須達下列材質標準：(詳細辦法依據國際田徑總會場地設施手冊)

| 測試項目 | 測試方法 | 國際田徑總會所規定之 跑道材質標準 |
| --- | --- | --- |
| 厚度 | 設施手冊3.1.3.3 | 13 mm |
| 吸震力 Force Reduction | 設施手冊3.1.3.4 | 35% ~ 50 % (10℃～40℃) |
| 垂直形變 Vertical Deformation | 設施手冊3.1.3.5 | 0.6mm～2.5mm (10℃～40℃) |
| 摩擦力 Friction | 設施手冊3.1.3.6 | ≧0.5 |
| 抗拉強度 Tensile Strenght | 設施手冊3.1.3.7 | ≧0.5 MPa |
| 伸長形變 ELONGATION AT BREAK | 設施手冊3.1.3.7 | ≧40 % |

- 認可之實驗室：跑道面層須經過國際田徑總會認可之任一實驗室做測試，且所有測試過程

(方法)應依照國際田徑總會規定進行。國際田徑總會承認之實驗室如下：

國際田徑總會承認之跑道面層實驗室一覽表(資料來源：IAAF Certification System – Procedure p.6-7, June 2016)

| CST- Centre for Sports Technology Unit 3, Greenwich Centre Business Park 53 Norman Road London SE10 9QF, Great Britain & N.I. Tel: +44 20 8293 6655 Rep: Graeme Tipp LRSC FIM LondonCST@aol.com | IST- Institut für Sportbodentechnik Hauptstrasse 34 CH-8264 Eschenz, Switzerland Tel: +41 52 740 30 05 Rep: Dipl.-Ing. Hans-Jörg Kolitzus hjkolitzus@bluewin.ch |
| --- | --- |
| IVB - Instituto de Biomecanica de Valencia Universidad Politécnica de Valencia - Edificio 9C, Camino de Vera s/n E-46022 Valencia, Spain Tel: +34 96 111 11 70 Rep: Sonia Gimeno Peña sonia.gimeno@ibv.upv.es | ISP - Institut für Sportstättenprüfung Südstrasse 1A D-49196 Bad Laer, Germany Tel: +49 (0) 5424 80 97 891 Rep: Dennis Frank D.Frank@ISP-Germany.com |
| Jiangsu Zhongzheng Testing Co., Ltd No. 818 Room, No.108 HeFeng Road, HuaQiao Town, KunShan City, Jiangsu 215332, China Tel: +86-512-36857685 Rep: Clark Lau, Mike Qian clark.lau@global-otc.com mike.qian@global-otc.com | MPA – University of Stuttgart Section 55150 “Sport surfaces, sports facilities” Pfaffenwaldring 32 (location 4g) D-70569 Stuttgart, Germany Tel: +49 711 685 62258 Rep: Dr.Ing. Karim Hariri Karim.hariri@mpa.uni-stuttgart.de |
| Kiwa ISA Sport Papendallaan 7, Postbus 721 6816 VD Arnhem, The Netherlands Tel: +31 26 483 46 37 Rep: Gert-Jan Kieft info.isa-sport@kiwa.nl | Österreichisches Forschungsinstitut für Chemie & Technik OFI Technologie & Innovation GmbH Arsenal Objekt 213, Franz Grill-Strasse 5, A-1030 Wien, Austria Tel: +43 1 798 1601-610 Rep: Dr.-Ing. Walter Müller walter.mueller@ofi.at |
| Labosport Technoparc Circuit des 24 Heures du Mans Chemin aux Boeufs 72100 Le Mans, France Tel: +33 2 43470840 Rep: Aurelien Le Blan contact@labosport.com | Sports Labs Ltd. 1 Adam Square, Brucefield Park, Livingston EH54 9DE, Great Britain & N.I. Tel: +44 0845 602 6354 Rep: Eric O’Donnell info@sportslabs.co.uk |
| Labosport Italia S.r.l. Via Monza, 80 23870 Cernusco Lombardone Lecco, Italy Tel: +39 039 896 2684 Rep: Roberto Armeni Roberto.armeni@labosport.it | USSL - United States Sports Surfacing Laboratory 548 Mary Esther Cutoff NW, Suite 18 - 320 Fort Walton Beach, FL 32548, USA Tel: +1 804 541 7212 Rep: Kathleen Smith ksmith@ussl-testing.com |
| Labosport UK Ltd. Unit 3, Aerial Way, Hucknall Business Park, Watnall Road, Hucknall, Nottingham England, N615 6DW United Kingdom Tel: +44 0 115 968 1968 Rep: Colin Young colin.young@labosport.co.uk |  |